PolySilicon Series Precision Thin-Film

Capacitors – Format “A”

Features:	Applications:

	Ultra-low profile (0.18 mm height)

	Dual topside wire-bonding pads

	Superior breakdown voltage performance

	High quality LPCVD nitride dielectric

	Capacitances from  20pF to 750pF

	Topside passivation for pick-and-place handling

	RoHS compliant and Pb-free

	125 kHz proximity access cards

	135 kHz RFID transponders

	Multi-chip-module (MCM)

	Chip-on-Board (COB) designs

	System-in-Package (SIP) designs

	Known Good Die (KGD) programs

	Chip and wire applications

Product Description

The SiliconApps SAPC capacitors use state-of-the-art semiconductor wafer manufacturing process to achieve an extremely stable and low-profile thin-film capacitor based on a silicon nitride (Si3N4) dielectric.  The capacitors are optimized for cost-sensitive applications where low profile and precision capacitance are required, such as 125 kHz security access card applications and RFID resonance circuits.

Each capacitor has two topside wire-bonding sites to support Chip-on-Board (COB) and Direct Chip Attachment (DCA) manufacturing flows.  The capacitor comprises of a silicon nitride dielectric between a polysilicon lower electrode and an aluminum top electrode. This combination results in outstanding reliability and excellent stability over

temperature.

An electrically isolated silicon substrate provides mechanical strength while allowing the use of either conductive or non- conductive die attach. The capacitors are passivated with an additional silicon nitride topside layer to protect the die during

Pick and place handling. Custom capacitor layout, values and

tolerances are available as

special orders.

The available Capacitance (C)

range for this format is 20pF to

750pF. The Breakdown Voltage (BV) varies depending on the capacitance value. The lower the C, higher the BV.

Electrical Specifications(1)

| Parameter | Symbol | Conditions |
| --- | --- | --- |
| Capacitance | C | 1 MHz, 1 V rms, 100% electrically tested |
| Temperature Coefficient of Capacitance | TCC | +45 ±25 ppm/°C |
| Operating Temperature Range | TOP | -55°C to +125°C |
| Insulation Resistance | IR | > 1010 ohms |
| Aging | AR | No aging effect |
| Working Voltage | WV | Maximum continuous operating voltage |
| Breakdown Voltage | VBR | > 1.5 X Working Voltage |

(1)  All measurements at 25°C unless otherwise specified

| ORDERING PART NUMBER |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| SAPC | 330 | K | 7 | A | W |
| Product Family | 3-digit Capacitance Code | Capacitor Tolerance | Device Thickness | Back Metal for Die Attach (Typical thickness) | Package Type |
|  | Capacitance Code Examples: 068 = 68pF and 510 = 510pF | J = ±5% | 9 = 9 mils | No Letter = Bare Silicon (No Back Metal) | W = Unsawn full 5" wafer |
|  |  | K = ±10% | 7 = 7 mils | A= Ti/Ni/Au (550A/4,000A/2,500A) | B = Diced and shipped on mylar/tape in Saw rings |
|  |  | M = ±20% | 6 = 6 mils | S = Ti/Ag (550A/5,000A) | P = Diced and shipped in Gelpak |

Part Number Example: SiliconApps SAPC330K7AW is a PolySilicon Capacitor; 330pF ±10%;

having 7-mils thick with Ti/Ni/Au back-metal and shipped as unsawn wafer

| Physical Dimensions |  |  |  |
| --- | --- | --- | --- |
| Parameter | Symbol | Dimension | Units |
| Capacitor Length (typical) (2) | L | 0.94 / (0.0370) | mm / (inches) |
| Capacitor Width ( typical) (2) | W | 0.88 / (0.0346) | mm / (inches) |
| Capacitor Thickness | T | 0.18 ±0.02 / (0.0071) | mm / (inches) |
| Die Stepping Distance on Wafer in X Direction | XSTEP | 990 | microns |
| Die Stepping Distance on Wafer in Y Direction | YSTEP | 930 | microns |

(2)   Final L, W dimensions depend on conditions and equipment used for wafer sawing. Values shown above reflect a 50 micron wide kerf.

| Bond Pad Coordinates |  |  |  |  |
| --- | --- | --- | --- | --- |
| Pad | Parameter | X | Y | Units |
| Pad A | (3) Center of Bond Pad | -260 | 275 | microns |
|  | Width of Passivation Opening | 250 | 150 | microns |
| Pad B | (3) Center of Bond Pad | 240 | 275 | microns |
|  | Width of Passivation Opening | 260 | 160 | microns |

(3)  Pad locations referenced to the center of the die. The +Y direction is away from the wafer flat